## Slide 1
Development of biodegradable spray mulch from lignosulfonate, chitosan, and biochar towards sustainable agriculture
Nitesh Kumar Kasera1, Sushil Adhikari1,2, Hossein Jahromi1
1 Department of Biosystems Engineering, Auburn University, Auburn, AL 36849
2 Center for Bioenergy and Bioproducts, Auburn University, Auburn, AL 36849
Materials and Methods
Introduction
Mulch preparation
Sample name and composition
Sample Name | L weight % | C weight % | BC weight % w.r.t. L
L100 | 100 | 0 | 0
C100 | 0 | 100 | 0
70L30C | 70 | 30 | 0
80L20C | 80 | 20 | 0
90L10C | 90 | 10 | 0
10BC | 80 (74.07) | 20 (18.52) | 10 (7.40)
20BC | 80 (68.97) | 20 (17.24) | 20 (13.79)
30BC | 80 (64.52) | 20 (16.13) | 30 (19.35)
L: Sodium Lignosulfonate, C: Chitosan, BC: Biochar; Overall weight % in parentheses |  |  | 
Performance testing
Characterization – Mechanical, Optical, Barrier, Thermal, Physicochemical
Performance evaluation – Sprayability, UV blocking, Moisture retention in soil
Results
Mulch properties
Mechanical properties:
Surface and barrier properties:
Optical properties:
Results
Mulch performance
Sprayability and moisture retention:
Photochemical stability:
Sample | Exposure Time (h) | Carbonyl Index (CI) | Increase in CI (%)
80L20C | 0 | 1.304 ± 0.25 | -
 | 4 | 1.624 ± 0.09 | 24.54
 | 8 | 1.740 ± 0.03 | 33.43
20BC | 0 | 1.524 ± 0.04 | -
 | 4 | 1.580 ± 0.13 | 3.67
 | 8 | 1.638 ± 0.06 | 7.48
Biodegradability:
What is mulch?
Protective layer on top-soil
Enables farmers to curtail the effects of drought, water loss, and soil erosion on crop production
History of mulch a
Problem and solution
The mulch photos in the first section of the Introduction are taken from Adobe Stock images, licensed by Auburn University
a Image is modified from Mansoor et al. (2022); Polymers Use as Mulch Films in Agriculture—A Review of History, Problems and Current Trends, Polymers, 2022, 14(23), 5062
The work was funded by the Alabama Agricultural Experiment Station at Auburn University through AgRSEED Program
Metrics | Plastic mulch | Bio-based mulch
Feedstock | Fossil-based | Renewable
Processing | 160 – 220 o C | < 40 o C
Application | Film laying | Spray applied
Retrieval | Needed | Not needed
Biodegradation | No | Yes
Soil health | Deteriorates | Improves